## Slide 1: Dislocations

## Slide 2: Dislocations
Burgers circuit & vector
Edge dislocation: line normal to slide
Dislocation glide under shear is the most frequent mechanism whereby metals are irreversibly deformed (plastic deformation)
Edge type
Shear along Burgers vector

## Slide 3: Dislocations
Dislocation line parallel to Burgers vector and to shear direction
Screw type

## Slide 4
Metals deform plastically via dislocation motion
Compression test on nano-pillar in single grain
Mixed dislocation line inside a grain gliding on a slip plane
Deformation under tension of single crystal along slip planes

## Slide 5
Edge dislocation interacting with SIA loop at 600 K
What happens when a dislocation meets a loop
Courtesy of L. Malerba and D. Terentyev (SCK-CEN)

## Slide 6: Shearable obstacles

## Slide 7: Shearable obstacles

## Slide 8: Shearable (weak) obstacles
Dislocations can cut through the obstacle: the bigger, the more difficult to cut it through
Elastic, chemical, and phase stability effects also play a role to determine obstacle strength
Increasing strain ‘chops up’ sheareable obstacles

## Slide 9: Impenetrable obstacles

## Slide 10: Impenetrable obstacles

## Slide 11: Impenetrable obstacles
The bigger the spacing between obstacles, the easier for the dislocation to squeeze through the gaps.
Each ‘bypass’ event leaves a dislocation loop behind, narrowing the gaps and increasing hardening.
Orowan loop

## Slide 12: Orowan loops are NOT ‘prismatic’ loops
Orowan loops
Interstitial-type prismatic loop
Vacancy-type prismatic loop

## Slide 13: Why does the yield strength increase after irradiation?
pinned dislocation
applied shear
Defect populations act as obstacles for dislocations

## Slide 14: Dislocations pinned by obstacles: the movie
In-situ straining TEM – Courtesy Prof. Matsui

## Slide 15: Take home messages
Dislocations are defects that always exist in metals (and other materials) and make irreversible (plastic) deformation possible
  This is why metals are ductile: they can deform before breaking
The yield strength is the stress to be applied to make dislocations move in a material
The presence of defects (loops, voids, precipitates, …) from irradiation makes dislocation glide more difficult  the yield strength increases, the material becomes harder