## Slide 1: Summary of modelling - and an example

## Slide 2: Radiation effects are inherently a multiscale problem
10s of nm = 10-8 m
100s of nm = 10-7 m
Length scale
ns = 10-9 s ….. ms = 10-3 s ….. 1 s …… 103 s
1 fs = 10-15 s
1-100 ps = 10-12- 10-10 s
Time scale
Precipitates
Loops & Cavities
Atomistic KMC
Nucleation &
Growth of
Precipitates &
Large Clusters
Defect
Migration
Secondary
Defect
Formation
Relaxation
Thermal spike
Collisions
Displacement
Cascade
Molecular dynamics
Incident particles
From n spectrum to PKA & Displacement Cascade Spectrum

## Slide 3
Component lifetime management
cm = 10-2 m
Length scale
10s of m = 10-5 m
s = 10-3 s.........................…………………….…… Years = 107 - 109 s
Time scale
Mechanical
Property Changes
Dislo/Defect Interaction
Yield Strength Increase
Loss of ductility
pinned dislocation
applied shear
Stress
Strain (%)
Increasing dose
Object KMC, rate theory
Growing Concentration of Radiation Induced Defects
while the Irradiation Proceeds
Dislocation dynamics
Bridge to crystal plasticity
Radiation effects are inherently a multiscale problem

## Slide 4: Modern approaches to materials modelling
Detailed Microstructural Examination
DFT
Nanostructure and microchemical evolution models
Conceptual model
MODEL
Interatomic Potential
Energy parameters
Molecular dynamics or other atomistic simulations
Mechanisms and additional parameters
Validation
Interpretation
Phenomena, Mechanisms

## Slide 5: An example of bottom-up understanding

## Slide 6
Slowing down is a non-monotonic function of Cr concentration
600 K
ln(DSIA clusterFeCr/DSIA clusterFe)
Atomic-level models show that 1D-migrating SIA clusters are slowed down in Fe-Cr alloys

## Slide 7
Fe irradiated with ions at 300°C: loops are formed, move and disappear to the surface

Fe8%Cr irradiated with ions at 300°C: loops are formed, but move much less and accumulate

Courtesy of M. Hernàndez Mayoral, CIEMAT
Electron microscopy confirms loop slowing down

## Slide 8
Little & Stow JNM, 87 (1979) 25
Reduced SIA cluster mobility, especially 1D migrating
Enhanced recombination with Cr-unaffected vacancies
Reduction of swelling
600 K
ln(DSIA clusterFeCr/DSIA clusterFe)
Swelling is a non-monotonic function of %Cr, too

## Slide 9
Enhanced recombination proven by positron annihilation spectroscopy
Positron annihilation studies show that total amount of vacancies in n-irradiated FeCr alloys decreases with Cr content
vacancy
SIA cluster
0.06 dpa
Lambrecht, PhD thesis, 2009
Fe

## Slide 10
0.06 dpa
Lambrecht, PhD thesis, 2009
FeCr
Enhanced recombination proven by positron annihilation spectroscopy
Positron annihilation studies show that total amount of vacancies in n-irradiated FeCr alloys decreases with Cr content

## Slide 11
0.06 dpa
Lambrecht, PhD thesis, 2009
Enhanced recombination proven by positron annihilation spectroscopy
Positron annihilation studies show that total amount of vacancies in n-irradiated FeCr alloys decreases with Cr content
These mechanisms, when properly parameterised, can be introduced in a rate theory or in kinetic Monte Carlo model which should provide a quantitative prediction of the actual concentration of point-defects and their clusters

## Slide 12: However, the comparison between models and experiments is not always easy …

## Slide 13: “Experimental validation”
Build a picture: Simulation results
?
Assumptions
Monte Carlo result
Atomistic results

## Slide 14: “Experimental validation”
Build a picture: Experimental result
???

## Slide 15: “Experimental validation”
God-like view