## Slide 1: Swelling
Courtesy of Lorenzo Malebra, SCK-CEN

## Slide 2: What is swelling?
Hardly any swelling is expected in LWRs
  ‘low’ temperatures
Effect will be important in GenIV reactors
  temperatures of 400°C to 700°C
  flux ≈ 100 flux LWR
After irradiation
Before irradiation

## Slide 3: Consequences of swelling
Annealed wire wrap spacer used on fuel pins assemblies in BN-600 (Russian sodium-cooled fast breeder reactor) – before irradiation
Spiral wrapped wire
Chuev, Lanskykh, Ogorodov, Sheikmann, Sergeev, 2004

## Slide 4: Consequences of swelling
Annealed wire wrap spacer used on fuel pins assemblies in BN-600 (Russian sodium-cooled fast breeder reactor) – after irradiation
Chuev, Lanskykh, Ogorodov, Sheikmann, Sergeev, 2004
Wire swelled more than cladding.

## Slide 5: What is swelling really?
5
Voids observed in a cold-worked 316 stainless steel baffle bolt from Tihange 1 (Belgian nuclear power plant) Thomas and Bruemmer, 2002
8.5 dpa, ~299ºC
Hardly any macroscopic swelling observed

## Slide 6: What is swelling really?
6
Voids observed in stainless steel after 73 dpa at 335ºC in BN-350 sodium fast reactor (Kazakhstan) Porollo, Konobeev, Garner, 2000
1.4 x 10-6 dpa/sec
6.2% swelling

## Slide 7: Another consequence of swelling: Void-induced embrittlement
7
Porter and Garner, 1988
14% swelling in 316 stainless steel irradiated at ~400ºC
Failure occurred during clamping at room temperature.

## Slide 8: Which variables affect swelling?
Steady-state swelling rate:
Almost material’s constant eventually always reached in steels: 1%/dpa (austenitics); 0.2%/dpa (F/M)
Transient regime:
Material and composition
Phase distribution
Temperature
Dpa-rate
Stresses
Incubation dose

## Slide 9: How can we explain swelling ?
Vacancies and self-interstitials are produced in the same quantity by neutrons
  Why only/mainly voids are observed in swollen metals ?
  What happened with the self-interstitials?
Volume seems to increase if voids are formed inside the material
  Voids in themselves decrease the macrosopic volume
  But how was matter removed from the voids and brought somewhere else?

## Slide 10: Dynamic bias
Self-interstitials migrate faster than vacancies
Self-interstitial
Vacancy
CV
Time (dose)
Concentration
CSIA
At steady state, more SIAs disappear at sinks than vacancies
So vacancy concentration is higher

## Slide 11: Dislocation bias
Self-interstitials interact at larger distance than vacancies with dislocations
They are absorbed more efficiently than vacancies
This leads to an even larger difference in concentration of the two species
SIA
vacancy
Dislocation line
Capture radius for SIA
rSIA
rV
Capture radius for vacancy

## Slide 12: Production bias
Vacancies are produced at the core of the cascade
SIAs are produced at the periphery of the cascade, in fairly large clusters
Vacancy clusters diffuse very slowly in 3D
SIA clusters diffuse fast in 1D
 Separation of the two populations

## Slide 13: A plausible mechanism for swelling
Swelling =
Transport of matter from bulk to sinks with cavity creation
<111> (bcc) or <110> (fcc)
sink
void
SIA cluster (loop)
cascade

## Slide 14: Void lattices
A pattern of voids can appear after high dose neutron irradiation – with the same structure as the underlying lattice!

## Slide 15: Take home messages
Swelling is a macroscopic change of volume observed in irradiated materials under certain conditions, generally accompanied by observation of voids inside the material
Versus dose, it is characterised by a transient regime and a steady state regime
  Extension of transient regime (incubation dose) depends on many variables: type of material, composition, phase distribution, temperature, dpa-rate, stresses, …
  Steady-state regime swelling rate is more or less a materials constant always reached eventually
Swelling can be explained in terms of biases, i.e. different properties of vacancy and SIA type defects leading to a partition of the two populations, with SIAs absorbed at sinks and vacancies forming voids inside the materials